GUIDE SPECIFICATION FOR PERMINATOR™ 15 MIL

UNDERSLAB VAPOR MAT

SECTION 07160

UNDERSLAB VAPOR RETARDER

Specifier Notes: This guide specification is written according to the Construction Specifications Institute (CSI) Format. The section must be carefully reviewed and edited by the Architect or Engineer to meet the requirements of the project. Coordinate this section with other specification sections and the drawings.

Specifier Notes: W.R. Meadows PERMINATOR™ Underslab Vapor Retarders are a new generation of resin/chemical technologies. They are vapor retarders created to provide the vaporproofing industry with economical, highly effective methods for preventing the penetration through the slab of damaging alkaline salts, moisture, mold, radon gas and water vapor.

PART 1 GENERAL

1.01	SECTION INCLUDES

A.	Surface preparation.

B.	Application of an underslab vapor retarder.

1.02	RELATED SECTIONS

Specifier Notes: Edit the list of related sections as required for the project. List other sections dealing with work directly related to this section.

A.	Section 03300 - Concrete.

B.	Section 07100 - Membrane Waterproofing.

C.	Section 09641 - Wood Strip Flooring.

D.	Section 09642 - Wood Parquet Flooring.

E.	Section 09643 - Resilient Wood Flooring System.

F.	Section 09651 - Resilient Tile Flooring.

G.	Section 09652 - Resilient Sheet Flooring.

1.03	REFERENCES

A.	American Society for Testing and Materials (ASTM)

1.	ASTM E1745 Standard Specification for Plastic Water Vapor Retarders Used in 			Contact with Soil Or Granular Fill Under Concrete Slabs.

2.	ASTM E154 Standard Test Methods for Water Vapor Retarders Used in Contact 			with Earth Under Concrete Slabs.

3.	ASTM E96 Standard Test Methods for Water Vapor Transmission of Materials.

4.	ASTM E1643 Standard Practice for Installation of Water Vapor Retarders Used in 		Contact with Earth or Granular Fill Under Concrete Slabs.

5.	ASTM F1249-01 Standard Test Method for Water Vapor Transmission Rate Through Plastic Film and Sheeting Using a Modulated Infrared Sensor.

B.  	American Concrete Institute (ACI)

1.	ACI 302.1R-96 Vapor Barrier Component (plastic membrane) is not less than 10 			mils thick.

1.04	SUBMITTALS

A.	Comply with Section 01330 - Submittal Procedures.

B.	Submit manufacturer's product data and application instructions.

1.05	DELIVERY, STORAGE, AND HANDLING

A.	Deliver materials to site in manufacturer's original, unopened containers and packaging, with 	labels clearly identifying product name and manufacturer.

B.	Store materials in a clean dry area in accordance with manufacturer's instructions.

C.	Stack membrane on smooth ground or wood platform to eliminate warping.

D.	Protect materials during handling and application to prevent damage or contamination.

E.	Ensure membrane is stamped with manufacturer’s name, product name and membrane thickness at intervals of no more than 85” (220 cm).

1.06	ENVIRONMENTAL REQUIREMENTS

A.	Product not intended for uses subject to abuse or permanent exposure to the elements.

B.	Do not apply on frozen ground.

PART 2	 PRODUCTS

2.01	MANUFACTURER

A.	W.R. Meadows, Inc., PO Box 338, Hampshire, Illinois 60140-0338. (800) 342-5976. (847) 		683-4500. Fax (847) 683-4544. Web Site www.wrmeadows.com.

2.02	MATERIALS

A.	Plastic Vapor Retarder

1.	Performance Based Specification:  Vapor Retarder membrane must meet or exceed 			all requirements of ASTM E1745 Classes A, B, & C.

a.  	Maximum Permeance ASTM E96:  0.018 Perms

b.	Water Vapor Transmission Rate ASTM F1249 calibrated to ASTM E96 (water method):  0.007 grains/ft2/hr

c. 	Resistance to Organisms and Substrates in Contact with Soil

ASTM E154, Section 13:  0.027 Perms

d.  	Tensile Strength ASTM E154, Section 9:  84 LBS. Force/Inch

e.  	Puncture Resistance	ASTM D1709, Method B:  4,335 Grams

f.  	Water Vapor Retarder ASTM E1745:  Meets or exceeds Class A, B & C

g.   	Thickness of Retarder (plastic) ACI 302.1R-96:  Not less than 10 mils

2.  	Proprietary Based Specification

a.  	Perminator™ 15 mil by W.R. Meadows.

b.	Stego-Wrap 15 mil by Stego Industries.

2.03	ACCESSORIES

A.	Seam Tape

1.	High Density Polyethylene Tape with pressure sensitive adhesive.  Minimum width 4 		inches.

B.  	Pipe Boots

1.	Construct pipe boots from vapor barrier material and pressure sensitive tape per 			manufacturer’s instructions.

PART 3 EXECUTION

3.01	EXAMINATION

A.	Examine surfaces to receive membrane. Notify Architect if surfaces are not acceptable. Do 		not begin surface preparation or application until unacceptable conditions have been 			corrected.

3.02	SURFACE PREPARATION

A.	Prepare surfaces in accordance with manufacturers instructions.

3.03	APPLICATION

A.	Installation shall be in accordance with manufacturer’s instructions and ASTM E 1643–98.

B.	Unroll vapor barrier with the longest dimension parallel with the direction of the pour.

C.	Lap vapor barrier over footings and seal to foundation walls.

D.	Overlap joints 6 inches and seal with manufacturer’s tape.

E.	Seal all penetrations (including pipes) with manufacturer’s pipe boot.

F.	No penetration of the vapor barrier is allowed except for reinforcing steel and permanent 	utilities.

G.	Repair damaged areas by cutting patches of vapor barrier, overlapping damaged area 6 			inches and taping all four sides with tape.

END OF SECTION